T-SHIRT, UNISEX (SHORT SLEEVE)

RME (ORANGE)

1   Scope

This specification covers the materials and make of T-shirts for Transnet Limited.

NOTES

1)  The following requirements will be specified in tender invitations and in each order or contract:

a)  the size(s) required (see 4.4).

2)  Special conditions of tender (that cover the conditions of acceptance of the T-shirts) are given in annex A.

2   Normative references

The following standards contain provisions which, through reference in this text, constitute provisions of this specification. All standards are subject to revision and, since any reference to a standard is deemed to be a reference to the latest edition of that standard, parties to agreements based on this specification are encouraged to take steps to ensure the use of the most recent editions of the standards listed below. Information on currently valid national and international standards may be obtained from the South African Bureau of Standards.

CSS 286.21,  Clothing ── LAB/1: Labelling ── PAC/1: Packing and marking.

CKS 129,  Colours for textiles.

SANS 877,  Woven cotton tapes.

SANS 1360-1,  Size designation of clothes ── Part 1: Men's and boys' outerwear garments.

SANS 1362,  Sewing threads.

SANS 10371  Terms and definitions for clothing.

SANS 5278  Sewing stitches per length.

SANS 105 B02,  Colour fastness to artificial light: Xenon arc fading lamp test..

SANS 105 C10,  Colour fastness to washing: Test 3.

SANS 105 E04,  Colour fastness to perspiration.

SANS 79,  Mass per unit area of conditioned textile fabrics.

SANS 5275,  Wales and courses per unit length in knitted textile fabrics (counting glass method).

SANS 960,  Dimensional changes of textile fabrics during washing.

SANS 6104,  Stitch length of weft-knitted fabrics.

SANS 10101, Standard nomenclature for stitches, seam and stitching’s

SANS 10188, Standard methods of garment measurement.

3   Definitions

For the purposes of this specification, the relevant definitions given in SABS 04 and the following definitions apply:

3.1  acceptable: Acceptable to Transnet Limited.

3.2  nominal: Subject to the tolerances normal to good manufacturing practice.

4   Requirements

4.1   Materials

4.1.1  General

The materials specified in 4.1.2 to 4.1.6 shall be supplied and used by the manufacturer. The colour of the stay tape and the sewing thread shall be an acceptable match to the colour of the knitted fabric.

4.1.2  Knitted fabric

The knitted fabric shall comply with the requirements given in table 1. The colour shall be an acceptable match to colour No. 149c-92 Stewart blue" 1) or an orange colour acceptable to Transnet Limited, both of CKS 129 (see reference item number in the title).

Table 1 - Knitted fabric requirements

| 1 | 2 | 3 |
| --- | --- | --- |
| Property | Requirement | Method of test |
| Composition Construction Courses per 10 cm, min. Wales per 10 cm, min. Stitch length, mm, max. Mass per unit area, g/m, min. Dimensional changes on washing, %, max. Length Width Colour fastness to light, rating, min. Colour fastness to washing, rating, min. Change in colour Staining of transfer cloths Colour fastness to perspiration, rating, min. Change in colour Staining of transfer cloths | 100 % Cotton Plain jersey 160 120 3,0 190 10 10 5 4 4 4 4 | Microscopically examination and chemical analysis Visual examination SANS SM 275 SANS SM 275 SANS SM 1104 SANS SM 79 SANS SM 960 Procedure A11) SANS ISO 105 BO2 SANS ISO 105 CO3 SANS ISO 105 EO4 |
| 1) Test in tubular form and tumble dry for 20 min at 70C. |  |  |

4.1.3  Neck and cuff binding

The binding shall be made from the knitted fabric and shall be of finished width 20 mm, after sewing to the neck and cuff openings.

4.1.4  Stay tape

A tape that complies with the requirements for type TA13 of SANS 877.

4.1.5 Embroidery thread

An acceptable 100% viscose embroidery thread of colours that are acceptable matches to colours

No. 873c- 99 Embroidery red and No. 507c-96  Navy of CKS 129.

4.1.6  Sewing thread

The sewing thread shall comply with the relevant requirements of SABS 1362 and shall be a polyester-and-cotton core-spun thread, ticket No. 120.

4.2  Workmanship

The T-shirts shall be made with first-class workmanship throughout and shall be free from defects that affect their appearance or may affect their serviceability (or both), and from marks, spots and stains incurred in the making up. All seams shall be smooth and all stitching uniform and free from twists, pleats and puckers and shall be sufficiently extensible to obviate seam cracking and undue shrinkage in use. All ends of sewing that are not secured in seams or other sewing shall be adequately back-tacked. All ends of sewing shall have been trimmed and loose threads removed. The T-shirts shall be of uniform and acceptable make, colour and finish.

4.3  Style

The T-shirt shall have a round neck and short sleeves and a logo on the left front.

4.4  Sizes

The T-shirts shall be supplied in one or more of the size designations given in column 1 of table 2, as specified in the order or contract, and their measurements, determined in accordance with figure 3, shall conform to the appropriate values given in columns 2 to 5.

Table 2 – Size range

| 1 | 2 | 4 | 5 | 6 | 7 | 8 | 9 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Size designation 1) | Nominal finished garment measurements, cm |  |  |  |  |  |  |
|  | Chest | ½ Hem | Back length | Back Width | Neck Circum. | Sleeve Under-arm | Cuff |
| 72-77 (XS) | 90 | 45 | 70 | 36 | 36 | 18 | 38 |
| 82-87 (S) | 100 | 50 | 74 | 40 | 38 | 18 | 40 |
| 92-97 (M) | 110 | 55 | 77 | 44 | 40 | 19 | 42 |
| 102-107 (L) | 120 | 60 | 80 | 48 | 42 | 19 | 44 |
| 112-117 (XL) | 130 | 65 | 82 | 52 | 44 | 20 | 46 |
| 122-127 (2XL) | 140 | 70 | 84 | 56 | 46 | 20 | 48 |
| 132-137 (3XL) | 150 | 75 | 86 | 60 | 48 | 21 | 50 |
| 142-147 (4XL) | 160 | 80 | 88 | 64 | 50 | 21 | 52 |
| 152-157 (5XL) | 170 | 85 | 88 | 68 | 52 | 22 | 54 |
| 162-157 (6XL) | 180 | 90 | 88 | 72 | 54 | 22 | 56 |
| 1) Based, on the chest girth, in centimeters, of the intended wearer. |  |  |  |  |  |  |  |

4.5  Make

NOTE ── Unless inconsistent with the text, all measurements are nominal.

4.5.1  Body

The body shall consist of two parts (i.e. a front and a back) that are seamed together at the sides and shoulders. The lower edge of the body shall have a hem of finished width 20 mm. Each shoulder shall be stayed on the inside with stay tape (see 4.1.4) that is sewn in with the shoulder seam.

4.5.2  Neck opening

The neck opening shall be round and shall be bound with binding (see 4.1.3). The binding shall be neatly closed on the left side (as worn) in line with the shoulder seam.

4.5.3  Sleeves

The sleeves shall be one-piece set-in short sleeves that are seamed under the arms. The ends of the sleeves shall be bound with binding (see 4.1.3). The binding shall be neatly closed in line with the seam.

4.5.4  Logos

4.5.4.1 Embroidered logo

Each T-shirt shall have the appropriate logo embroidered on the chest on the left front (see figure 1). The colour of the screen-printing shall be an acceptable match to colour No. 1c-95 "White" of CKS 129.

4.6   Stitches, seams and stitching’s

4.6.1 General

All sewing shall be in accordance with SABS 0101.

4.6.2  Stitches

The stitches shall be as follows:

a) bound edges: stitch type 402 or other acceptable stitch type;

b) hem: stitch type 502 or type 503 or other acceptable type of overlocking stitch; and

c) all other sewing: stitch type 504 or other acceptable type of overlocking stitch.

4.6.3  Seams

The seams shall be as follows:

a) bound edges: seam type BSb; and

b) all other seams: seam type SSa.

TRANSNET

Manufacturer’s name

ITEM NO:

35/000000

Size: 97 cm

Spec. No:  G201

100% Cotton

MADE IN SOUTH AFRICA

Y.O.M   2020

VAT No: 0000000

4.6.4  Stitchings

Stitching type EFl.

4.6.5  Number of stitches

40  4 per 10 cm.

5   Labelling, packing and marking

5.1   Labelling       As specified in CSS 286.21 LAB/1.

5.2   Packing and marking     As specified in CSS 286.21 PAC/1.

Figure 1 – Position of Logo

| Size designation | 72 | 77 | 82 | 87 | 92 | 97 | 102 | 107 | 112 | 117 | 122 | 127 | 132 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dimensions "X", cm | 11.75 | 12 | 12.25 | 12.75 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 16.5 |

| Measuring Points | Description |
| --- | --- |
| A-A : Chest circumference | Measure at the base of the armhole, with the garment spread completely flat, and multiply by 2. |
| B-B : Neck circumference | Measure across the width of the neck opening at the neck seam, with the seam straight but not stretched, and multiply by 2. |
| A-C : Underarm sleeve length | Measure from the base of the armhole to the bottom edge of the cuff. |
| D-D : Back length | Measure from the neck binding to the bottom hem, including the binding. |

Annex A

(normative)

Special conditions of tender

A-1   Unless otherwise stated, Transnet Limited (or an officer or organization deputed by it), shall be the inspecting authority.

A-2   Three pre-production sample T-shirts, and at least two square metres of the knitted fabric clearly marked with the dye batch, shall have been inspected, tested and approved by the inspecting authority before bulk production is commenced and it shall be the duty of the manufacturer to give adequate notice to the inspecting authority of the availability of these samples. The samples shall each be accompanied by a trim chart containing a sample of each component material (as given in 4.1.4 to 4.1.6). From time to time, further samples will also be drawn during consignment inspections for destruction testing.

NOTE - When new dye batches of yarn are to be used in production, a sample piece of the knitted fabric, with the dye batch clearly marked, shall be tested and approved by the inspecting authority before the dye batch may be used in production.

A-3   The T-shirts shall be subject to inspection during the course of manufacture. The inspector shall, during normal working hours, be given all reasonable facilities for carrying out his duties and shall have the right of entry into the contractor's factory and the factory or works of any subcontractor where work on T-shirts supplied to this specification may be in progress.

A-4   The contractor shall inspect the finished T-shirts for compliance with the specification before submitting them to the inspecting authority for final inspection.

A-5    Before acceptance, the T-shirts shall have been inspected and tested by the inspecting authority and found to comply with the requirements of the specification.

| REVISION HISTORY SHEET |  |  |
| --- | --- | --- |
| Document Quality Assurance Subject ADMINISTRATION, PREPARATION, MAINTENANCE AND DISTRIBUTION |  |  |
| Approving Officer: C. du Plooy |  |  |
| Rev/No | Date approved | Nature of revision |